# Board specification

Board name:	ADX412-EVM Rev C

Number and revision: 	106-000-009 Rev C

Special features: 	The board layout is rotated 20 degrees to make critical high-frequency traces run at an angle relative to the glass fiber weave to improve high frequency matching. Please do not rotate the layout back when placed on the panel.

Number of layers: 	8

Board type: 	FR4, RoHS compliant

Board thickness: 	1.6 mm +/- 10%

Board size: 	160 mm x 100 mm (+/- 0.25 mm)

Surface plating: 	Immersion Ag

Surface mount 	Top and bottom

Electical test: 	Yes

Minimum trace width: 	0.1 mm

Minimum clearance: 	0.1 mm

Minimum hole size: 	0.3 mm

Miminum annular ring: 	0.3 mm (pad diameter - hole diameter):

Solder mask: 	Liquid Photo Imageable, green color

Plugged vias: 	Some of the 0.3 mm vias are covered by solder mask while others are not. This is intentional to enable access by test probes to some vias. (Bigger vias are not plugged.)

Silk screen: 	Top and bottom, white color
Please remove silk screen print that is too close to or directly over solder pads.

Copper thickness outer layers: 	35-45 um (target: 42 um)

Copper thickness inner layers: 	18-45 um (target: 33 um)

# Layer Stackup

Solder mask

Copper layer 1

Prepreg 0.19 mm

Copper layer 2

Core 0.19 mm

Copper layer 3

Prepreg 0.19 mm

Copper layer 4

Core 0.19 mm

Copper layer 5

Prepreg 0.19 mm

Copper layer 6

Core 0.19 mm

Copper layer 7

Prepreg 0.19 mm

Copper layer 8

Solder mask

# Controlled Impedance

There are a number of traces where the delay is critical. Since it does not seem possible to

ask for a specific propagation speed I instead ask for controlled impedance. The traces that

are important are located on the top layer and the bottom layer (microstrip). They are of two

types, differential pairs and single-ended lines. Ground reference planes are located on the adjacent

layer.

The differential microstrips that need controlled impedance have a width of 0.1 mm with 0.1 mm

isolation. Target differential impedance is 100 ohms.

The single ended microstrips that need controlled impedance have a width of 0.31 mm. Target

impedance is 50 ohms.

# Supplied files

Gerber file format:	274X, mm, 4:3, suppress leading zeros

Drill file format:	Excellon, mm, 4:3, suppress leading zeros